

6753 Chestnut Ridge Road

Beach City, OH 44608

To:

Reference: Manufacturer’s Certification (00 45 46)

Dear \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_:

This is to certify that the siding insulation and accessories to be provided for the referenced project comply with the specified requirements:

UL 723/ASTM E 84

a. Flame Spread Index: 5.

b. Smoke Developed Index: 100 to 200.

ASTM C 303

1. Density: 1.0 pcf (16 kg/m3).

ASTM C 272: (Water Absorption):

1. Maximum 2.75 percent by volume.

ASTM E 96 (Water Vapor Transmission):

1. 5.0 perms/inch.

ASTM C 578: Thermal Expansion:

1. 0.000035 inch/inch/degree F (0.000063 mm/mm/degree C).

Third-party testing certification of these results is available upon request.

Sincerely,

Patrick Culpepper, President

Progressive Foam Technologies, Inc.